Degradation-Aware Physics-Guided Hybrid Transfer Learning for Cross-Batch State-of-Health Prediction of Lithium-Ion Batteries

Jichao Zhuang1, *, Jiaming Yang1

1 School of Mechanical and Electrical Engineering, Guangzhou University, Guangzhou 510006, China

*Corresponding author: J. Zhuang (zjc_10242021@gzhu.edu.cn).

Abstract

State-of-health (SOH) prediction models trained on historical lithium-ion battery batches often show reduced performance on a new batch. This reduction can arise from distribution shifts, inconsistent degradation stages, and cell-to-cell variation. To address these challenges, we propose a degradation-aware physics-guided hybrid transfer learning framework for cross-batch SOH prediction. The framework first adopts a physical-residual SOH modeling strategy, where a low-order nonlinear degradation prior captures the global capacity-fade trend while a residual temporal module learns cell-specific local deviations from this trend. A degradation-state-guided curve attention temporal aggregation mechanism then incorporates the estimated degradation state and local voltage-curve morphology into temporal feature aggregation. This mechanism adjusts the emphasis on local temporal segments across degradation stages. We further introduce lifecycle-indexed, degradation-aware maximum mean discrepancy (MMD) regularization to support feature transfer between the source and target domains. Estimated SOH serves as a degradation-state indicator that dynamically adjusts alignment strength and increases the cross-domain constraint at lower SOH levels. Experiments on a lithium-ion battery dataset show that the framework provides competitive prediction errors relative to the representative recent methods evaluated here. Ablation studies further demonstrate the contribution of each proposed module.

Keywords

Lithium-ion battery, State of health. Cross-batch prediction, Physics-guided learning, Transfer learning

1 Introduction

Lithium-ion batteries are widely used in electric vehicles, energy-storage systems, and portable electronics because of their high energy density, long cycle life, and low self-discharge rate. As cyclic aging accumulates, batteries often exhibit capacity fade and internal-resistance growth, which can compromise system safety and reliability. Accurate estimation of battery state of health (SOH) is therefore one of the central tasks in battery management[1].

Data-driven SOH estimation methods have advanced in recent years. Representative approaches include multimodel fusion[2]，data augmentation[3]，graph neural networks[4]and hybrid feature networks[5].These methods seek to improve predictive accuracy and robustness. However, many rely on broadly consistent data distributions between the training and test domains. When batteries come from different production batches or operating conditions, cross-domain shifts can limit transfer of the learned mapping. The resulting loss of generalization may be substantial.

Transfer learning has become an important approach for addressing distribution shifts in cross-battery SOH estimation. Existing studies have introduced strategies such as domain adaptation[6]， meta-learning[7]，deep transfer learning[8] and transfer ensemble learning[9]to mitigate limited target-domain labels and cross-domain distribution discrepancies.However, most of these methods still learn the SOH mapping in a purely data-driven manner, requiring the model to simultaneously capture the global degradation trend, local degradation patterns, and cross-domain feature alignment. When target samples are scarce and degradation trajectories differ significantly, the model may struggle with such complex mapping, leading to limited prediction accuracy.

Notably, physics-guided modeling has increasingly become an important direction for improving the reliability of SOH estimation. Researchers have introduced physics-informed neural networks[10], physical constraints[11],domain-knowledge fusion[12] and degradation-feature optimization[13], which combine battery degradation mechanisms with data-driven models to enhance the physical consistency of SOH prediction. However, existing methods tend to emphasize physical priors and local degradation information, without adequately addressing the distribution shift problem in cross-batch prediction. A unified modeling framework that integrates global degradation trend constraints, local residual learning, and cross-domain feature alignment is still lacking, which limits the cross-domain generalization capability of these models.

To address the above challenges, this work focuses on cross-batch SOH prediction for lithium-ion batteries under a common data system, and proposes a degradation-aware physics-guided hybrid transfer learning framework. First, a physical-residual SOH modeling strategy is constructed. It employs a low-order nonlinear degradation prior to capture the global capacity-fade trend, while a residual temporal module learns cell-specific local deviations from this trend. Furthermore, a degradation-state-guided curve attention temporal aggregation module is developed. This module activates the temporal feature aggregation between the estimated degradation state and the local voltage-curve morphology, thereby enhancing the representation of stage-wise changes and local fluctuations in the SOH curve. To mitigate cross-domain distribution discrepancies, a lifecycle-indexed degradation-aware MMD regularization strategy is proposed. It dynamically strengthens the cross-domain feature alignment as the estimated SOH decreases, thus tightening the distribution constraint at deep degradation stages and improving the domain adaptation capability for cross-batch SOH prediction.

The main contributions are as follows.

(1) We introduce a physical-residual SOH modeling strategy. A low-order nonlinear prior captures the global degradation trend, while a residual temporal network learns local cell-specific deviations. This hybrid design avoids a purely black-box SOH mapping.

(2) We construct a degradation-state-guided curve attention temporal aggregation mechanism. The estimated degradation state and local voltage-curve morphology are jointly incorporated into the temporal feature aggregation process, enabling the model to adjust its attention to local temporal segments across different degradation stages. This mechanism enhances the representation of stage-dependent changes and local fluctuations in the SOH curve.

(3) We design a lifecycle-indexed degradation-aware MMD regularization strategy. The estimated SOH dynamically adjusts the cross-batch feature alignment strength, imposing a stronger distribution constraint between source and target domains as degradation progresses. This regularizer provides a complementary domain-adaptation mechanism for cross-batch SOH prediction.

2 Related works

2.1 Lithium-ion battery SOH estimation

The essence of lithium-ion battery SOH estimation lies in establishing a mapping between battery cycling information and capacity retention. In recent years, data-driven methods have gradually replaced health-indicator-based modeling approaches, automatically learning battery degradation patterns from voltage curves, capacity changes, partial charge–discharge segments, and multiscale health features[14–16].With the development of deep learning, SOH estimation has further shifted from manually designed features to end-to-end representation learning[17,18].However, such methods typically rely on the assumption that the source and target domains share similar data distributions. To avoid this assumption, transfer learning has been introduced into SOH estimation. To address the inconsistency between source and target feature spaces, Zhang et al. employed MMD-assisted feature alignment, improving the capability of battery health estimation under one-shot conditions[19]. Given source domain，and target domain，transfer learning seeks to adapt source-domain health representations to the target domain, as illustrated in Fig. 1. A general objective is

where  is the source-domain SOH regression loss, ， is the adaptation constraint between domains, and， is a balancing coefficient.

Existing cross-batch studies have examined lightweight transfer learning[20]， few-shot transfer learning [21] and time-frequency domain adaptation [22]. However, when target-domain samples are limited and degradation-stage coverage is incomplete, the direct mappingmay increase prediction instability during late-stage degradation. Cross-batch SOH prediction therefore requires both a transfer mechanism and a suitable degradation-trend prior that structurally constrains the output.

Fig.1 Conceptual comparison between source-only SOH estimation and transfer-learning-based SOH estimation

2.2 Physics-constrained SOH estimation

Physical constraints can not only suppress overfitting of deep networks under small sample sizes, but also introduce physical knowledge, domain priors, and distribution constraints into SOH prediction, as illustrated in Fig. 2. In general, physical embedding can be formulated as jointly feeding the original observed features and physics-prior features into the prediction model, and adding a corresponding physical constraint term to the training objective:

Where  denotes observed battery-degradation features,  denotes features constructed from physical knowledge or degradation priors, andis a physical-consistency or degradation constraint.

Recent studies have successively incorporated physical knowledge, hybrid modeling, and degradation-feature constraints into the SOH estimation process[23–26]. By combining empirical degradation regularities with data-driven models, these approaches have improved both the accuracy and physical consistency of SOH prediction. In addition, methods such as feature selection, diagnostic-test design, and generative learning [3,27–29] introduce degradation priors from different perspectives to enhance model robustness under complex data distributions. However, most existing methods focus on specific physical priors or local degradation information, while paying insufficient attention to the distribution shifts in cross-batch prediction. A framework that unifies degradation-trend constraints and cross-domain feature alignment is still lacking. Therefore, how to exploit physical priors to structurally constrain the transfer learning process remains an urgent problem to be solved in cross-batch SOH prediction.

Fig.2 Schematic view of regularized learning for battery SOH prediction

3 Methodology

3.1 Problem definition

给定第个由单循环充电电压轨迹和循环位置信息组成的样本，其中充电电压轨迹经线性插值重采样为长度为的一维序列，循环位置记为。采用Nominal SOH作为预测目标，其定义如下，其中表示第个循环对应的放电容量，指得是额定容量。进一步的，循环位置归一化方式表示为，其中为归一化尺度。因此，模型的基本输入可定义为。跨批次SOH预测的目标是学习一个映射函数，使其能够在源域与目标域的共同约束下，给出稳定的SOH估计，其中表示模型参数。

3.2 总体框架

提出一种degradation-aware physics-guided hybrid transfer learning框架，用于跨批次锂电池SOH预测。该框架主要包括physical-residual SOH建模策略、退化状态引导的曲线注意力时序聚合机制以及生命周期指数退化感知MMD正则化策略，如图3所示。具体而言，首先利用归一化循环位置构建低阶非线性退化先验，并采用残差时序模块学习单体电池相对于全局退化趋势的局部退化偏差，从而形成physical-residual SOH建模策略。进一步地，设计一种退化状态引导的曲线注意力时序聚合机制，使模型能够根据不同退化阶段调整对局部序列片段的关注程度。最后，设计一种生命周期指数退化感知MMD正则化策略提高跨批次特征一致性约束。

从图4发现，将SOH预测表示为低阶退化先验与数据驱动残差校正项的叠加，

其中，表示低阶非线性退化先验，是残差项，指的是残差网络参数。此外，模型训练目标由SOH回归损失与特征对齐正则项组成，其整体形式为，

其中，为回归损失，为源域与目标域间的退化感知正则损失，为平衡系数。

Fig.3 Overall framework

3.3 Physical-residual SOH modeling

We decompose battery SOH degradation into a shared trend and cell-specific local deviations. This decomposition reduces the burden of fitting the entire SOH curve with a neural network. A low-order nonlinear prior first represents the global capacity-fade trend over cycling. The residual temporal module then compensates for local deviations that the prior cannot describe.

3.3.1 低阶非线性退化先验构建

锂离子电池容量在循环过程中通常呈现非线性衰减趋势，但不同电池个体在局部阶段仍存在一定退化差异。若完全依赖神经网络直接学习 SOH 变化过程，模型需要同时拟合全局退化趋势、局部退化波动以及跨批次分布差异，容易增加学习复杂度并削弱模型的物理一致性。为此，从低阶函数投影的角度构建非线性退化先验，将归一化循环位置映射到一个低维退化基函数空间中，以获得共享 SOH 参考基线。

给定第  个样本的归一化循环位置 ，定义低阶退化基函数向量为，

相应的，低阶非线性退化先验可表示为该基函数向量与系数向量间的投影关系，

其中，，、、、 为待优化系数。上述四个系数共同决定退化基线的初始偏移、整体下降趋势以及非线性弯曲形态，使模型以较少参数描述 SOH 曲线的变化趋势。

为进一步说明低阶非线性退化先验的构建过程，对、、、 四个系数的优化景观进行可视化。从图 4 可知，最终拟合得到的系数组合均位于低 RMSE 增量区域内，且最优邻域呈现连续的误差变化趋势，说明该低阶基函数投影能够以有限参数形成相对稳定的全局退化参考。由此，后续残差时序模块无需直接拟合完整 SOH 曲线，可进一步聚焦于不同电池单体相对于该参考曲线的局部退化偏离。

Fig.4. Pairwise optimization landscape of the four coefficients in the low-order nonlinear degradation prior

In each panel, two coefficients are varied while the other two are fixed at their source-domain least-squares optimum. The color denotes the RMSE increase relative to the optimal coefficient solution, and the red point indicates the fitted coefficient pair. The coefficient optimization is performed using only Batch 1-8 source-domain training samples.

为避免目标测试批次信息参与先验构建，低阶退化先验的系数仅根据源域训练样本进行拟合。设表示源域训练样本集合，表示对应真实 SOH，则系数优化过程可写为，

等价地，上述过程可理解为在低阶退化基函数空间中求解源域 SOH 观测在最小二乘意义下的投影函数 ，以刻画源域样本中可由低阶非线性基函数表示的共享退化趋势。通过该优化过程，模型首先吸收可由低阶非线性基函数表达的共享退化成分，再将剩余的个体化局部偏差交由残差时序模块学习，从而通过低阶退化先验建立具有明确结构含义的全局锚点。

3.3.2 残差时序建模

在低阶退化先验的基础上，不同电池单体仍会受到制造偏差、循环工况以及批次差异等因素的影响，表现出相对于全局退化趋势的个体化偏离。为刻画难以由低阶退化先验描述的局部退化特征，进一步构建残差时序模块，使模型学习真实SOH与低阶退化先验间的残差映射。具体而言，对于第个样本，其残差目标定义为，

残差网络的输出表示为，

因此，SOH预测结果可写为，

其中， 表示网络学习得到的局部残差校正项。残差分支采用一维卷积提取充电电压轨迹中的局部时序特征，并通过循环单元对重构后的序列表示进行建模，以学习电池退化过程中的长期时序依赖关系。其过程可表示为，

其中，表示一维卷积，为局部电压轨迹特征，是循环单元，为输出的序列特征。该残差建模方式将全局退化趋势与局部退化偏差解耦，使模型无需直接拟合完整SOH曲线，而是关注个体化退化模式。

3.4 Degradation-state-guided Curve Attention for Temporal Aggregation

在 residual temporal branch 中，充电电压轨迹经过局部卷积与循环单元编码后，可得到一组时序隐状态表示。对于第 i 个样本，该序列表示记为，

其中，表示第 t 个局部时序位置的隐状态，T 为序列长度。常规注意力机制通常仅依据  计算各位置的重要性，难以区分不同退化阶段下局部曲线片段对 SOH 估计的贡献差异。为此，构建一种degradation-state-guided curve attention 机制，在时序聚合过程中建立退化状态向量与曲线局部形态 token，使模型能够根据电池当前退化水平对局部时序信息进行自适应聚焦，如图 5 所示。

Fig.5 Flowchart of degradation-state-guided curve attention for temporal aggregation

首先，根据归一化循环位置及低阶非线性退化先验输出构造退化状态向量，

其中， 表示归一化循环位置， 表示由低阶非线性退化先验得到的全局退化参考值， 用于表征相对退化程度。该状态向量不直接替代电压轨迹特征，而是作为注意力计算中的条件信息，用于描述样本所处的退化阶段。

同时，为补充隐藏状态中可能被平滑的局部曲线变化信息，基于电压轨迹构造曲线形态 token，

其中，表示第 t 个位置的电压值，与 分别表示其一阶与二阶局部变化项。公式（17）用于刻画电压曲线的局部水平、斜率变化以及弯曲形态，为后续注意力分配提供曲线形态约束。

在此基础上，退化状态向量被映射为阶段条件查询向量，

随后，结合时序隐状态、曲线形态 token 以及阶段条件查询向量计算第 t 个位置的注意力得分，

其中，、 和  为可学习参数。与仅依赖隐状态的注意力不同，公式（19）使注意力得分同时受到三类信息的约束。具体而言， 提供残差分支学习到的时序退化表征， 提供电压曲线的局部形态信息， 则提供与退化阶段相关的条件引导。

进一步地，为避免不同退化阶段采用固定的注意力分布 sharpness，开发了一种退化状态相关的温度参数，

其中， 为温度下界，为可学习参数。公式（20）使注意力分布的集中程度能够随退化状态进行调整。当样本处于不同循环阶段或不同估计退化水平时，模型可在较平缓的全局聚合与较集中的局部聚焦间自适应切换。

最后，利用带温度调节的归一化权重对时序隐状态进行聚合，

其中，表示第 t 个局部位置的注意力权重， 为聚合后的残差时序表示，并输入后续回归层以获得残差校正项。该模块作为 physical-residual SOH 建模策略中的辅助表示单元，有助于模型在保持整体结构简洁的同时，增强对关键局部退化片段的表达能力。

Fig.6. Mechanistic visualization of degradation-state-guided adaptive curve attention

图6展示了退化状态引导曲线注意力机制的内部响应。图a代表性电压曲线 token 及其注意力高亮位置，橙色短线表示该阶段内注意力较高的局部片段。图b为不同退化阶段的平均注意力分布，晚期阶段的注意力峰值更加集中。图c为随循环归一化位置增加，注意力温度与熵整体下降，表明模型在退化加剧时采用更尖锐的聚焦策略。图d-f为在固定晚期退化状态与隐藏上下文后，展示电压水平 V、斜率 ΔV 以及曲率 Δ²V 对注意力兼容性的响应面。黑色散点为锂电池晚期高注意力 curve token，橙色点为注意力加权中心。

3.5 生命周期指数退化感知MMD正则化策略

在跨批次SOH预测中，源域历史批次与目标新批次间通常存在特征分布偏移。尽管不同批次电池遵守相似的整体退化规律，但其充电电压轨迹、容量衰减速率以及阶段性退化特征仍存在显著差异，从而影响模型的跨域泛化。为解决上述问题，在训练阶段构建生命周期指数感知MMD（Maximum Mean Discrepancy）正则化策略，对源域与目标域的潜在特征分布进行约束，以缩小跨批次特征分布差异，如图7所示。

Fig.7 Mechanism of degradation-aware MMD regularization for cross-batch feature alignment

给定源域融合特征集合与目标域融合特征集合，通过MMD度量两域在再生核希尔伯特空间中的均值嵌入，其一般形式可表示为，

其中，表示特征映射，为再生核希尔伯特空间。基于核函数展开后，MMD可写为，

其中，为核函数。采用多核高斯核以增强不同尺度下的分布差异刻画能力，

传统MMD对不同退化阶段施加相同强度的对齐约束，难以反应电池退化过程中跨批次分布偏移的阶段差异。考虑到电池低SOH阶段通常表现出更显著的退化不确定性与批次间差异，进一步构建指数退化感知权重，使跨域特征对齐强度能够随目标域估计SOH的降低而增强。具体而言，对于一个训练batch，目标域的平均SOH表示为，

基于该退化状态，指数退化感知权重定义为，

其中，为退化感知系数。最终的退化感知MMD正则项可表示为，

因此，整体训练损失为，

其中，第一项为源域SOH监督损失，第二项为源域与目标域间的退化感知特征对齐正则项。

Fig.8 Training trajectories of unweighted and degradation-aware weighted MMD losses

The gray dashed curve denotes the static MMD loss without degradation-dependent weighting, while the blue curve denotes the exponential degradation-aware weighted MMD loss. The shaded region represents mean ± s.e.m. over three random seeds. The highlighted interval corresponds to the MMD-guided training stage, and the inset magnifies the late active window.

为进一步说明指数退化权重对 MMD 正则项训练行为的影响，图 8给出了无权重 MMD 与指数退化感知加权 MMD 的 loss 轨迹对比。可以看到，在 MMD 引导训练区间内，两类 MMD loss 均随训练过程逐步下降。相比无权重 MMD，加权 MMD 在后期退化阶段保持更低的对齐损失水平。该结果说明，指数退化权重并未改变 MMD 的基本度量形式，而是在训练过程中调节跨批次特征对齐强度，使模型在退化程度较高的阶段获得更充分的分布约束。

3.6 Implementation Details

模型以长度为 100 的充电电压轨迹与归一化循环位置作为输入，其中低阶非线性退化先验的系数仅在源域训练样本上拟合。第一、二层的残差分支的将输入通道分别映射为 16、32个特征通道，其中两层均采用 kernel size 为 3 的一维卷积，并结合 batch normalization、ReLU 激活以及最大池化。同时，循环单元的隐藏维度设置为 64。注意力模块同时接收时序隐状态、退化状态向量以及由电压值、一阶差分以及二阶差分构成的曲线形态 token。退化状态向量由归一化循环位置、低阶退化先验输出及相对退化程度组成。模型训练采用 Adam 优化器，初始学习率设置为 ，batch size 设置为 128，总训练轮数为 150，更多超参数细节见表1。MMD 外层权重设置为 ，退化感知系数设置为。所提方法的整体训练流程如算法1所示。

TABLE1. Implementation settings and hyperparameters

| Category | Parameter | Setting | Description |
| --- | --- | --- | --- |
| Input | Voltage sequence | 100 points | Interpolated charging-voltage trajectory |
| Input | Cycle position | Normalized p | Used for degradation prior and statevector |
| Physical prior | Prior form | Cubic polynomial | Fitted using source-domain samples |
| CNN block | Conv. channels | 16->32 | Local voltage feature extraction |
| CNN block | Kernel/ pooling | k = 3; MaxPool(2) | Applied in each convolutional block |
| Temporal encoder | Recurrent unit | Hidden size =64 | Encodes local temporal states |
| Attention | State vector | dim=3 | [p,y_base, 1 -y_base] |
| Attention | Curve token | dim=3 | [V, Delta V, Delta^2 V] |
| Regression head | Dropout | 0.2 | Used before residual SOH regression |
| Optimizer | Optimizer | Adam | Applied to all trainable modules |
| Training | Epochs /batch size | 150/128 | Fixed for all retained experiments |
| Learning rate | Initial/decay | 1e-3; x0.1 at epoch 100 | Late-stage training stabilization |
| MMD regularization | Active epochs | 21-120 | Warm-up and sprint stages exclude MMD |
| MMD regularization | lambda_mmd / gamma | 5e-5/5.5 | Outer MMD weight and degradation factor |

4 实验与分析

4.1 数据集描述

采用Huazhong Artificial Intelligence Lab发布的公开锂离子电池数据集。该数据集包含77个商业电池单体，在不同放电协议下形成超过140000个充放电循环样本。数据划分在电池批次完成，其中Batch 1-8作为源域，包含61个电池与115256 个样本。Batch 9作为目标域，包含8个电池与16310个样本。Batch 10作为最终盲测集，包含8个电池与14556个样本，如表1所报道。图9展示了该数据集的可视化。为了量化实验结果，采用 Average RMSE、MAE以及MAPE作为评价指标。此外，考虑到不同电池的循环长度差异，仅采用上述指标容易受到样本数量较多电池的影响。因此，进一步采用Macro RMSE评估模型在不同电池上的平均预测误差。设Batch 10中共有个电池，第个电池包含个循环样本，则Macro RMSE定义为，

其中，与分别表示第个电池中第个循环样本的真实SOH与预测SOH。

Fig.9 Overview of the lithium-ion battery dataset and representative voltage-current degradation signals

TABLE 2 Fixed cross-batch split summary

| split | samples | cells | batches | xshape | ymin | ymax |
| --- | --- | --- | --- | --- | --- | --- |
| source | 115256 | 61 | 1,2,3,4,5,6,7,8 | 115256x100 | 0.799 | 1.119 |
| targetadapt | 16310 | 8 | 9 | 16310x100 | 0.800 | 1.113 |
| targettest | 14556 | 8 | 10 | 14556x100 | 0.799 | 1.122 |

4.2 SOH预测

从表3中可清晰发现，所提出方法取得 Average RMSE 为 0.009278，macro RMSE 为 0.008216，MAE 为 0.005733，以及MAPE 为 0.614%。从误差量级看，该结果约对应 0.95% SOH 的 Average RMSE，说明模型能够在未参与训练与checkpoint 选择的新批次电池上保持较低的整体预测误差。进一步观察每个 Batch 10 电池的预测曲线可知，所提方法在多数电池上能够跟随 SOH的下降趋势，尤其在高 SOH 与中间退化阶段具有较好的轨迹跟踪能力，如图10所示。该结果表明，低阶退化先验与残差时序模块的组合能够在整体退化趋势与局部偏差间形成互补，使模型不完全依赖神经网络直接拟合完整 SOH 曲线。

Fig. 10 Batch10 per-cell SOH prediction curves

表3 SOH预测的度量结果

| Battery Index | n | RMSE | MAE | MAPE(%) |
| --- | --- | --- | --- | --- |
| 69 | 1702 | 0.011899 | 0.007875 | 0.845 |
| 70 | 1697 | 0.006143 | 0.004690 | 0.495 |
| 71 | 1848 | 0.006891 | 0.004697 | 0.503 |
| 72 | 1811 | 0.005218 | 0.003429 | 0.369 |
| 73 | 2030 | 0.006332 | 0.003909 | 0.423 |
| 74 | 2285 | 0.016069 | 0.011457 | 1.226 |
| 75 | 1783 | 0.004801 | 0.003201 | 0.344 |
| 76 | 1400 | 0.008379 | 0.005268 | 0.565 |
| Average | 14556 | 0.009278 | 0.005733 | 0.614 |
| Macro mean | 8 | 0.008216 | 0.005566 | 0.596 |

图 11 给出了各测试单体的 RMSE 与 MAE 分布，用于更直观地观察模型在单体层面的误差变化。可以看出，除编号 10-6 的测试单体外，其余电池的 RMSE 均低于 1.20% SOH，MAE 均不超过 0.79% SOH。编号 10-7 的误差最低，其RMSE 与 MAE 分别为 0.48% SOH 与 0.32% SOH。相比之下，编号 10-6 的 RMSE 与 MAE 分别达到 1.61% SOH 与 1.15% SOH，是当前 Batch 10 中误差较高的单体。上述结果表明，所提出模型在多数目标测试电池上能够保持较低的单体级预测误差，但在个别电池上仍会受到单体差异和局部退化行为的影响。总体而言，模型不仅在 Average RMSE指标上取得较低误差，也在多数单体上保持了相对稳定的 SOH 回归表现。

Fig. 11 Per-cell RMSE and MAE distribution on the Batch 10 blind-test cells

4.3 与先进方法的对比

为验证所提方法的优越性，采用5种先进方法进行对比。具体而言，PINN4SOH 将 SOH 估计表示为物理信息神经网络约束下的退化动力学学习过程[30]。SSF-WL 通过弱标签自监督学习与 Transformer 编码器增强充电曲线表征[31]。AM-MFF 利用注意力机制对多源退化特征进行融合，以提高 SOH 估计的鲁棒性[32]。PIKAN通过自编码器与对抗学习构建跨域一致的隐空间健康特征，并采用最近邻相似性进行 SOH 赋值[33]。

如表 4 所示，所提出方法取得Average RMSE、Macro RMSE 以及 MAE 分别为 0.009278、0.008216 以及 0.005733，MAPE 为 0.614%的预测结果。所提方法的 RMSE 分别低于 PINN4SOH、SSF-WL 以及 AM-MFF 约 0.006659、0.009427 以及 0.006333，MAE 分别降低约 0.005432、0.007487 以及0.005174。该结果表明，仅依赖通用物理信息约束、弱标签序列表征以及多特征注意力融合，仍难以充分处理批次间退化轨迹差异。相比之下，低阶退化先验、残差时序学习与退化感知特征对齐的结合更有利于降低整体预测误差。

进一步的，图 12 对 RMSE 与 MAE 进行了可视化比较。可以看出，所提方法在整体误差指标上保持最低水平。PIKAN在输入由 relaxation voltage 特征适配为固定长度充电电压轨迹后误差明显增大，说明基于隐空间最近邻赋值的跨域估计方法对输入特征形式与目标域对齐质量较为敏感。

TABLE 4. Reproduced comparison with recent journal SOH estimation methods under the same cross-batch

| Method | RMSE | Macro RMSE | MAE | MAPE(%) |
| --- | --- | --- | --- | --- |
| Proposed | 0.9278 | 0.8216 | 0.5733 | 0.6143 |
| PINN4SOH | 1.5937 | 1.5088 | 1.1165 | 1.1735 |
| SSF-WL | 1.8705 | 1.8080 | 1.3220 | 1.4134 |
| AM-MFF | 1.5611 | 1.5007 | 1.0907 | 1.1540 |
| PIKAN | 7.5347 | 7.3958 | 5.4650 | 5.8582 |
| MSWaveFuser | 1.1480 | 1.0492 | 0.8209 | 0.8606 |

Fig. 12. Performance comparison of the proposed method and representative advanced SOH estimation methods

4.4 Comparison with baseline models

To verify the effectiveness of the proposed method, we compared it with seven baselines: CNN-LSTM, LSTM, GRU, PCA-GPR, PCA-RBF-SVR, PCA-LinearSVR, and the cubic degradation baseline. The results are shown in Figure 13. The proposed model achieved an Average RMSE of 0.009278, a Macro RMSE of 0.008216, and an MAE of 0.005733, outperforming all compared methods. CNN-LSTM yielded an RMSE of 0.016075, indicating that purely convolutional and recurrent end-to-end data-driven modeling struggles to adequately capture global degradation trend differences and batch shifts in the present cross-batch prediction task.

PCA-GPR and PCA-RBF-SVR can perform nonlinear regression on low-dimensional statistical features; however, their ability to represent the local degradation morphology of charging voltage trajectories remains limited. Notably, the cubic degradation baseline produced an RMSE of 0.032649, higher than that of the full model. This suggests that the low-order nonlinear degradation prior cannot independently replace temporal residual learning; its primary role is to provide a global degradation reference for the SOH curve. LSTM and GRU achieved RMSE values of 0.032742 and 0.033109, respectively, demonstrating that without the low-order degradation prior, local temporal aggregation, and target-domain alignment constraint, recurrent networks are prone to large prediction errors in cross-batch scenarios. Therefore, the advantage of the proposed method does not arise from a single structure but from the functional complementarity among its different modules.

Fig. 13 Main Batch10 baseline comparison

4.5 小样本实验

为了进一步分析目标域数据在跨批次 SOH 预测中的作用，设置了 source-only与不同目标开发电池数量的消融实验。source-only 表示模型仅利用 Batch 1-8 源域训练，不使用 Batch 9 目标开发电池进行特征对齐。其他设置则分别使用 1、2、4 以及 8 个 Batch 9 电池作为目标样本。

source-only 的RMSE 为 0.010805，而当使用8 个 Batch 9 电池时，RMSE 为 0.009448，如图14。该结果说明，有限目标开发数据能够为跨批次适应提供一定帮助。然而，不同目标开发样本数量的误差并未呈现严格单调下降趋势。使用 2 个目标电池的 RMSE 为 0.011190，高于 source-only。这说明目标数据的作用不仅取决于数量，也受到所选目标电池代表性与退化阶段覆盖情况的影响。Batch 9 目标域能够为模型选择与特征对齐提供参考，但在小样本条件下，其稳定性仍受到目标子集组成的影响。在模型复杂度方面，当前模型约包含 31466 个可训练参数，checkpoint 大小约为 0.391-0.392 MB，推理延迟约为 0.046 ms/sample。所提出方法在当前实验环境下具有较低的推理开销，能够在保持模型规模较小的同时完成跨批次 SOH 估计。

Fig. 14 Target-development budget sensitivity

4.6 消融实验

为分析不同模块对 SOH 预测性能的贡献，设计了消融实验，包括移除低阶非线性退化先验、 attention-assisted temporal aggregation、MMD 正则以及将指数退化感知 MMD 替换为 static MMD。

完整模型的RMSE 为 0.009499，如图15所示。移除低阶非线性退化先验后，RMSE 上升至 0.020716，MAE 上升至 0.013759，是所有消融项中退化最明显的消融。这说明低阶退化先验对跨批次 SOH 预测具有关键作用。移除 attention-assisted temporal aggregation 后，RMSE 上升至 0.011677，MAE 上升至 0.008145。该结果表明，attention 模块能够改善局部充电电压轨迹特征的聚合方式，对残差分支具有辅助贡献。但从误差变化幅度看，attention 的作用可描述为有效的辅助表征模块。此外，no-MMD 的 RMSE 为 0.009677，static MMD 的 RMSE 为 0.009635，指数退化感知 MMD 的 RMSE 为 0.009499。三者间的差距较小，说明 MMD 对预测精度的贡献有限。

Fig. 15 Ablation and static-MMD control

为进一步观察模型在不同退化阶段的表现，将 Batch 10的每个电池按照归一化循环位置划分为 early、mid 以及late 三个阶段，结果如图16所示。完整模型在 early、mid 以及late 阶段的 RMSE 分别为 0.003120、0.009111 以及0.013341。相比之下，移除低阶退化先验后 late-stage RMSE 上升至 0.031926，表明该先验对后期退化阶段的稳定预测具有较强作用。

Fig. 16 Stage-wise RMSE comparison

5 讨论

为了评估随机种子对模型的影响，进一步整理了 seed 7、seed 42 以及 seed 123 的多随机种子结果，结果如图17所示。移除低阶退化先验后的平均 RMSE 为 0.022364，明显高于完整模型与其他消融模型，进一步验证低阶退化先验的关键作用。同时，完整模型的三种子平均 RMSE 为 0.010381，而 no-MMD的三种子平均 RMSE 为 0.010249，二者差距很小且 no-MMD 的略低。这可归因于MMD 在当前证据下并不是稳健的预测精度来源。

Fig. 17 Multi-seed stability

尽管 MMD 对RMSE 的贡献较小，但表征预测结果仍显示其具有源域与目标域对齐作用。为解释该现象，如图18所示，使用源域 Batch 1-8 与目标域 Batch 9 的 fused SOH features 进行可视化，并考察特征 MMD^2、domain classifier AUC、PCA 主成分方向上的源-目标质心差异贡献以及归一化综合域差异指数。去除 MMD 约束后，源域与目标开发域融合特征在三维 PCA 空间中仍存在较明显的质心间隔，说明残差时序分支学习到的潜在表示中仍保留一定批次相关成分。引入指数退化感知 MMD 后，目标域特征整体向源域主特征流形靠近，域分类器可分性同步下降，表明该正则项能够在训练阶段压缩跨批次均值嵌入差异，并削弱与 SOH 回归无关的域识别信息。

进一步结合 PC 方向贡献可看出，MMD 的影响不只体现为距离指标降低，也表现为 fused SOH features 中源目标质心偏移的重新分配。该结果说明，MMD 作为迁移约束来解释跨批次表征一致性，为残差校正项提供更稳定的输入分布。

Fig. 18 Source-target representation diagnostic of the SOH transfer model.

(a) Dual-axis comparison of feature MMD^2 and domain-classifier AUC for the final model and ablated variants;

(b) PC1-PC3 contribution to the source-target centroid gap for the final and w/o MMD models;

(c) Three-dimensional PCA visualization of fused SOH features for the w/o MMD variant and the proposed model. Blue points denote source-domain samples, orange points denote Batch 9 target-development samples, and dashed lines denote source-target centroid gaps.

6 Conclusion

To address the susceptibility of lithium-ion battery SOH prediction models to distribution shifts, inconsistent degradation stages, and cell-specific deviations in cross-batch applications, a degradation-aware physics-guided hybrid transfer learning framework is proposed. The framework constructs a physical-residual SOH modeling strategy that uses a low-order nonlinear degradation prior and a residual temporal module to learn the global degradation trend and local deviations of different cells. A degradation-state-guided curve attention temporal aggregation mechanism is also developed, which incorporates the estimated degradation state and local charging-voltage-curve morphology into the residual feature aggregation process to dynamically adjust the model's attention to local temporal segments. Furthermore, a lifecycle-indexed degradation-aware MMD regularization is designed to constrain the feature alignment between source and target domains. Experimental results show that the proposed framework maintains low overall prediction errors on the lithium-ion battery dataset and achieves stable SOH regression on most tested cells. Ablation experiments verify the effectiveness of the global degradation prior, local residual learning, and cross-domain feature alignment. However, the current experiments are mainly based on cross-batch splits within the same dataset and have not yet covered generalization validation across different battery types. Future work will further incorporate multiple datasets, diverse operating conditions, and more complete degradation-stage coverage to build more broadly applicable battery health management methods.

Acknowledgments

References

[1]	Ma G, Xu S, Jiang B, Cheng C, Yang X, Shen Y, et al. Real-time personalized health status prediction of lithium-ion batteries using deep transfer learning. Energy Environ Sci 2022;15:4083–94. https://doi.org/10.1039/d2ee01676a.

[2]	Zhang Y, Wik T, Bergström J, Zou C. State of Health Estimation for Lithium-Ion Batteries Under Arbitrary Usage Using Data-Driven Multimodel Fusion. IEEE Trans Transp Electrif 2024;10:1494–507. https://doi.org/10.1109/TTE.2023.3267124.

[3]	Echabarri S, Do P. A modified TimeGAN-based data augmentation approach for the state of health prediction of Lithium-Ion Batteries. Reliab Eng Syst Saf 2025;264:111297. https://doi.org/10.1016/j.ress.2025.111297.

[4]	Zhou KQ, Qin Y, Yuen C. Graph neural network-based lithium-ion battery state of health estimation using partial discharging curve. J Energy Storage 2024;100:113502. https://doi.org/https://doi.org/10.1016/j.est.2024.113502.

[5]	Zhao Y, Geng L, Meng W, Meng J, Wu C, Hu X, et al. Cross-attention-based hybrid feature fusion network for state-of-health estimation of lithium-ion batteries. Sci Rep 2026;16:17800. https://doi.org/10.1038/s41598-026-48317-5.

[6]	Li H, Li X, Dong Y, Hang H, Tian Y, Tian J. A cross-material lithium-ion battery state of health estimation method based on three-stage domain adaptation. Energy 2025;341:139376. https://doi.org/10.1016/j.energy.2025.139376.

[7]	Zhao X, Wang Z, Han T, Yang W, Gu F, Ball AD. A Meta-Learning Method for Few-Shot Multidomain State-of-Health Estimation of Lithium-Ion Batteries. IEEE Trans Transp Electrif 2025;11:4830–40. https://doi.org/10.1109/TTE.2024.3470551.

[8]	Liu H, Deng Z, Che Y, Xu L, Wang B, Wang Z, et al. Big field data-driven battery pack health estimation for electric vehicles: A deep-fusion transfer learning approach. Mech Syst Signal Process 2024;218:111585. https://doi.org/https://doi.org/10.1016/j.ymssp.2024.111585.

[9]	Wu J, Cui X, Meng J, Peng J, Lin M. Data-Driven Transfer-Stacking-Based State of Health Estimation for Lithium-Ion Batteries. IEEE Trans Ind Electron 2024;71:604–14. https://doi.org/10.1109/TIE.2023.3247735.

[10]	Liu Y, Chen H, Yao L, Ding J, Chen S, Wang Z. A physics-guided approach for accurate battery SOH estimation using RCMHCRE and BatteryPINN. Adv Eng Informatics 2025;65:103211. https://doi.org/https://doi.org/10.1016/j.aei.2025.103211.

[11]	Wang F, Wu Z, Zhao Z, Zhai Z, Wang C, Chen X. Physical knowledge guided state of health estimation of lithium-ion battery with limited segment data. Reliab Eng Syst Saf 2024;251:110325. https://doi.org/https://doi.org/10.1016/j.ress.2024.110325.

[12]	Lanubile A, Bosoni P, Pozzato G, Allam A, Acquarone M, Onori S. Domain knowledge-guided machine learning framework for state of health estimation in Lithium-ion batteries. Commun Eng 2024:1–13. https://doi.org/10.1038/s44172-024-00304-2.

[13]	Su L, Tao S, Chen Y, Zou C, Zhang X. Incremental capacity feature selection for lithium-ion battery state of health estimation considering estimation capability and efficiency. Cell Reports Phys Sci 2026;7. https://doi.org/10.1016/j.xcrp.2025.103083.

[14]	Li X, Yu D, Vilsen SB, Jindal P, Subramanian VR, Stroe DI. Degradation analysis and tanks-in-series modeling of lithium-ion batteries with state of health-adaptive charging strategies. ETransportation 2026;28:100561. https://doi.org/https://doi.org/10.1016/j.etran.2026.100561.

[15]	Arbaoui S, Samet A, Ayadi A, Mesbahi T, Boné R. Data-driven strategy for state of health prediction and anomaly detection in lithium-ion batteries. Energy AI 2024;17:100413. https://doi.org/https://doi.org/10.1016/j.egyai.2024.100413.

[16]	Zhou Y, Wang S, Xie Y, Zeng J, Fernandez C. Remaining useful life prediction and state of health diagnosis of lithium-ion batteries with multiscale health features based on optimized CatBoost algorithm. Energy 2024;300:131575. https://doi.org/https://doi.org/10.1016/j.energy.2024.131575.

[17]	Wong KL, Tse R, Tang S-K, Pau G. Decentralized Deep-Learning Approach for Lithium-Ion Batteries State of Health Forecasting Using Federated Learning. IEEE Trans Transp Electrif 2024;10:8199–212. https://doi.org/10.1109/TTE.2024.3354551.

[18]	Ji X, Chen Y, Wang J, Zhou G, Sing Lai C, Dong Z. Time-Frequency Hybrid Neuromorphic Computing Architecture Development for Battery State-of-Health Estimation. IEEE Internet Things J 2024;11:39941–57. https://doi.org/10.1109/JIOT.2024.3448350.

[19]	Zhang M, Wang X, Kang L, Xie D, Liang B. Bridging the feature gap: Heterogeneous transfer learning for lithium-ion battery health estimation using one-shot data. Results Eng 2026;29:109163. https://doi.org/https://doi.org/10.1016/j.rineng.2026.109163.

[20]	Liu J, Member GS, Qin Y. A Lightweight Transfer Learning-Based State-of-Health Monitoring With Application to Lithium-Ion Batteries in Autonomous Air Vehicles. IEEE Trans Ind Informatics 2026;22:1738–49. https://doi.org/10.1109/TII.2025.3631012.

[21]	Song L, Gui X, Du J, Fan Z, Li M, Guo L. A Novel Transfer Learning Approach for State-of-Health Prediction of Lithium-Ion Batteries in the Absence of Run-to-Failure Data. IEEE Trans Instrum Meas 2024;73:1–12. https://doi.org/10.1109/TIM.2024.3450095.

[22]	Pang X, Zhang X, Guo Z, Jia J, Wen J, Shi Y, et al. TFDDA: a time-frequency deep domain adaptation method for cross-domain state of health estimation of lithium-ion batteries. Eng Res Express 2026;8:45210. https://doi.org/10.1088/2631-8695/ae43b2.

[23]	Nie X, Pan Y, Zhang Y, Luo Z, Wang S. Battery health prediction under data scarcity: A cross-domain physics-informed 5-shot framework with GRU-Transformer. Appl Energy 2026;402:127012. https://doi.org/https://doi.org/10.1016/j.apenergy.2025.127012.

[24]	Lin C, Tuo X, Wu L, Zhang G, Lyu Z, Zeng X. Physics-informed machine learning for accurate SOH estimation of lithium-ion batteries considering various temperatures and operating conditions. Energy 2025;318:134937. https://doi.org/https://doi.org/10.1016/j.energy.2025.134937.

[25]	Tian A, He L, Ding T, Dong K, Wang Y, Jiang J. A generic physics-informed neural network framework for lithium-ion batteries state of health estimation. Energy 2025;332:137215. https://doi.org/https://doi.org/10.1016/j.energy.2025.137215.

[26]	Tao S, Zhang M, Zhao Z, Li H, Ma R, Che Y, et al. Non-destructive degradation pattern decoupling for early battery trajectory prediction via physics-informed learning. Energy Environ Sci 2025;18:1544–59. https://doi.org/10.1039/d4ee03839h.

[27]	Du X, Meng J, Amirat Y, Gao F, Benbouzid M. Feature selection strategy optimization for lithium-ion battery state of health estimation under impedance uncertainties. J Energy Chem 2025;101:87–98. https://doi.org/https://doi.org/10.1016/j.jechem.2024.09.032.

[28]	Zhuang D, Li ML, Lam VN, Braatz RD, Chueh WC, Bazant MZ. Physics-Informed Design of Hybrid Pulse Power Characterization Tests for Rechargeable Batteries. J Electrochem Soc 2024;171:50510. https://doi.org/10.1149/1945-7111/ad4394.

[29]	Tao S, Guo R, Lee J, Moura S, Casals LC, Jiang S, et al. Immediate remaining capacity estimation of heterogeneous second-life lithium-ion batteries via deep generative transfer learning. Energy Environ Sci 2025;18:7413–26. https://doi.org/10.1039/d5ee02217g.

[30]	Wang F, Zhai Z, Zhao Z, Di Y, Chen X. Physics-informed neural network for lithium-ion battery degradation stable modeling and prognosis. Nat Commun 2024;15:4332. https://doi.org/10.1038/s41467-024-48779-z.

[31]	Wang T, Ma Z, Zou S, Chen Z, Wang P. Lithium-ion battery state-of-health estimation: A self-supervised framework incorporating weak labels. Appl Energy 2024;355:122332. https://doi.org/https://doi.org/10.1016/j.apenergy.2023.122332.

[32]	Chen S-Z, Liu J, Yuan H, Tao Y, Xu F, Yang L. AM-MFF: A multi-feature fusion framework based on attention mechanism for robust and interpretable lithium-ion battery state of health estimation. Appl Energy 2025;381:125116. https://doi.org/https://doi.org/10.1016/j.apenergy.2024.125116.

[33]	Dou B, Hou S, Li H, Zhao Y, Fan Y, Sun L, et al. Cross-domain state of health estimation for lithium-ion battery based on latent space consistency using few-unlabeled data. Energy 2025;320:135257. https://doi.org/https://doi.org/10.1016/j.energy.2025.135257.